Radiation embrittlement of reactor pressure vessel steels with a high nickel content

V. Revka (, E. Grynik, L. Chyrko, Yu. Chaikovsky

Radiation material science department, Institute for Nuclear Research, 47 Nauki, av., Kiev, 03628, Ukraine

Keywords: RPV steel, surveillance tests, radiation embrittlement, nickel, fracture toughness, Master curve

PACS classification codes: 61.82.Bg; 62.20.Mk

Abstract

The analysis of the Ukrainian NPP surveillance test results for the VVER-1000 reactor pressure vessel has been performed. A nickel effect on RPV material embrittlement was considered taking into account a manganese content. It is shown the radiation embrittlement rate for welds with a high nickel (> 1,5 % wt) and high manganese (> 0,8 % wt) content exceeds a normative value. Fracture toughness data for the RPV steels have been re-evaluated using the Master curve methodology. The conclusion was made the critical brittleness temperature shift due to irradiation, ∆ТF, may underestimate the fracture toughness curve shift. Furthermore, it has been demonstrated the PNAE G-7-002-86 normative approach characterizes highly conservatively the fracture toughness of some unirradiated RPV materials.

( Corresponding author. 	Tel.: +380 44 5254781; Fax: +380 44 5252620;

E-mail: grynik@kinr.kiev.ua