First
Intraband electron focusing in bilayer graphene
Csaba G. Péterfalvi1, László Oroszlány2, Colin J. Lambert1 and József Cserti2
1 – Lancaster University, UK; 2 – ELTE, Budapest, Hungary
New J. Phys. 14 063028 (2012)
http://iopscience.iop.org/1367-2630/14/6/063028
[Speaker Notes: I'm Cs P, ESR in Lancs Uni. Present our latest results about ~]

---
Outline
Outline
Trigonal warping in the low-energy band structure of BLG,
additional deformation by mechanical strain... =>
Changing topology and symmetry breaking in the spectrum!
- Inspiration: 'Flat-lens focusing of electrons on the surface of a topological insulator'
Hassler, Akhmerov and Beenakker, Phys. Rev. B 82, 125423 (2010)
- This can be done in graphene too!
  - probe the spectrum's topology and symmetries,
  - strain controlled electron flow,
  - strain detection,..
[Speaker Notes: First we'll review what we already know about the low-energy band structure of BLG, emphasising the trigonal warping effect and the effect of external strain on the spectrum of BLG. Inspired by the results of the Hassler—Akhmerov—Beenakker paper, we have calculated the electron flow semiclassically in a simple system with a point-like source and a planar scattering potential. In the second part, we'll discuss these results focusing on how mechanical distortion deforms the diffraction pattern. Concerning the possible applications, this electron optical phenomenon can be utilized in several ways. By scanning the electron density with an STM tip, one can probe the spectrum and tell about the topology, symmetries and the number of Dirac-points; and thus detect strain; or even control the electron-flow by strain. Now we shall start with the effective Hamiltonian.]

---
Hamiltonian
The Symmetry Breaking Hamiltonian
External electrostatic potential
Kinetic term from the 1st neighbour intralayer interaction
Complex scalar describing mechanical strain1
and also e-e interaction to some extent2...
Kinetic term from the 2nd neighbour interlayer interaction
Trigonal warping
ξ is the valley index > valleytronics
[1] M. Mucha-Kruczyński, Phys. Rev. B 84, 041404 (2011)
[2] Y. Lemonik, Phys. Rev. B 82, 201408 (2010)
[Speaker Notes: ...which breaks the usual symmetry attributed to graphene systems on higher energies. Let's go over the different terms in the 2x2 effective Hamiltonian... [A1] EESP – which will be a step-function in our case realizing a planar potential step. [A2] The usual kinetic term – still symmetic. [A3] Trigonal warping term breaks the rotational symmetry ~> anisotropy, also breaks the K-K' symmetry ~> valleytronics! [A4] w represents mechanical strain and also e-e interaction to some extent, but since the latter derivation is somewhat qualitative, we attribute w to mechanical deformation throughout our calculation.]

---
Contours
Energy contours
v3 deforms the band structure. Anisotropy! Trigonal warping!
Curvature is a function of E (or k) and also very sensitive to w.
solid: w = -6 meV; dashed: w = 0 meV; dotted w = 6 meV
w = 0 meV
Zooming close to the Dirac points...
[Speaker Notes: To find out what happens at low energies, zoom close to a K-point. In the inset the E-contours are presented around a K point. Note how the originally circular contours got deformed trigonally while lowering the energy[A1]: Ei,.. curvature change,.. Et,.. Lifshitz transition!.. Note that the originally quadratic minimum divided into four packets with linear Dirac-cones! In this figure w=0, which corresponds to the dashed curve in the main figure. Here [A2] the curvature is presented as the function of E along the k_x axis [that is this!]. The main message is that the curvature is energy-dependent and also very sensitive to w[: other curves]! We are interested in the region where the curvature changes sign. ~> Later on, our electrons will scatter from [this state] to [this state] with negative curvature [corresponding points in the subfig!], which is shown in more detail in the next slide...]

---
Contours 2
Consequences of the anisotropy?
Negative refraction at the potential step!..
Potential step and classical trajectories in real space
Dispersion curves and wavevectors in k-space
Group velocity’s direction ≠ wavevectors’ direction !
[Speaker Notes: This figure shows the basic idea behind our calculations. Here we displayed rays of electrons in real space and in the reciprocal space at the same time! [Show dispersion curves and the junction!] Let's follow the course of an electron from the point source S, with a wave vector denoted by the blue dashed line! Since the group velocity is perpendicular to the energy contour, it won't be parallel to the wave vector[A1] in this anisotropic system with noncircular energy contours. Because of the system's translational invariance along the junction, the parallel component of k must be conserved. This condition determines a point on a lower energy contour on the other side of the junction, corresponding to the refracted ray, as well as an other point on the left contour, corresponding to the reflected ray. Again, the group velocities will point normal to the contours. Note that the change of the curvature's sign, makes the refracted rays converge, which leads us to our next important observation[A2]: negative refraction occurs at the potetntial step! Let us see how it works exactly!..]

---
Negative n
About negative refraction...
[Speaker Notes: In the bottom left figure you can see the Source radiating a bunch of electrons close to the optical axis, and an other bunch at an angle to that. The trajectories meet again to the right of the junction in separate focal points. The corresponding wavevectors in k-space are there in the figures above. Please note the opposite curvatures. On the right, red lines denote the ratio of the energy contours' curvatures, and black lines the refractive index for the two sets of trajectories. Note that the condition for focusing is not a negative refractive index (n<0), but the sign change of the curvatures! (ci/ct<0) However, close to the optical axis these conditions are equivalent, and what's more, if the contours are symmetric to the optical axis, then n=ci/ct [point it out!].]

---
Setup
The experimental setup
[Speaker Notes: An experimental setup may look like this, with dimensions in the order of a couple of microns. On this scale, a point-like source-electrode can be defined on the x axis, emitting both K and K' electrons. At the junction, defining the y axis, particles disperse or focus depending on which valley they come from. On the right, an STM tip can be used to scan the electron density. The junction is steep enough to be treated step-like and smooth enough to avoid inter-valley scattering.]

---
Overall
The theoretical setup
In real space...
...and in k-space.
Rays get partially reflected
and refracted at the junction.
Electron from K’ focus, but
electrons from K diverge.
Valley selection, Valleytronics...
[Speaker Notes: The corresponding theoretical setup can be seen in this slide. [Here] you can see the energy contours around K and K', with blue arrows representing the incident electrons, green arrows the transmitted electrons and red arrows the reflected ones. The real-space trajectories clearly show that the K-electrons disperse, while the K'-electrons converge. We'll see later that the valley selection is close to perfect, in the local maxima, the electrons' valley-polarization is very high. By using semi-classical catastrophe optics, we summed up all the contributing electron rays coherently, and we've got the following results...]

---
Fig 'a
Total particle densities are calculated using semi-classical catastrophe optics.
Contributions of electron rays are summed up coherently.3
Dark blue lines are the theoretical curves of the cusp caustics.
Electrons from one valley constitute one bunch of local maxima.
The diffraction pattern rotates together with the lattice...
[3] K. M. Borysenko, Phys. Rev. B 83,
161402 (2011)
[Speaker Notes: In these figures, you can see the electron density to the right of the junction which is at the left edge of each subfigure. The six subfigures belong to six different values of 'a, which is the rotation angle of the lattice relative to the junction. [Dark blue lines] are the theoretical curves of cusp caustics, fitting nicely to the global maximum / focal point. Note that each bunch of local maxima is formed by electrons from the same valley, and the whole pattern of diffraction fringes rotates together with the lattice... // Catastrophe optics stems in catastrophe theory, which, in general, can deal with systems driven by a generator function seeking its stationary points. At certain coordinates in the parameter space, a slight change in external parameters can cause these stationary points to jump, and these sudden changes are referred to as catastrophes. In catastrophe optics, this generator function is the optical length. Thus caustics have the same structure as the standard catastrophes of the general theory. In this description, the nondivergent wavefunction is obtained in the form of a Fresnel–Kirchhoff-type diffraction integral, which has several advantages compared to the exact quantum mechanical solution: (i) it can be applied in systems of arbitrary geometry, not only with special symmetries, (ii) it enables caustics to be sorted into equivalence classes based on their structural stability, which allows much more insight into the physics of the phenomena, (iii) via the so-called universal scaling laws, the theory predicts how the pattern and the intensity relations of the caustics evolve in the asymptotic short wavelength limit, which also helps the full understanding of the problem, and finally (iv) in many cases, the semiclassical integral representation of the solution is much easier and faster to evaluate numerically than the exact results. Although catastrophe optics is rooted in topological concepts, the theory is not purely qualitative, and it can produce quantitative results, the accuracy of which increases in the short wavelength limit. It is worth emphasizing the basic difference between stable and unstable caustics: stable (typical) caustics usually occur in natural systems with low symmetry, while in contrast, unstable (atypical) caustics require artificial setups with high symmetry. Even though, in most of the cases, manmade devices with precise optical configuration still produce stable caustics, these are regarded as optical aberrations.]

---
Movie
[Speaker Notes: ...this pattern is periodic and repeats itself after 60 degrees. This is no surprise, since the trigonal energy contours around K rotated by 60 degrees, overlap those around K', and vice versa.]

---
Polarization
Polarization
[Speaker Notes: This figure shows the high degree of polarization of electrons in a single bunch of fringes. The colour blue means electrons from the K point, and red means electrons from K'. Note that the local maxima are either monochrome blue or red, which means, the polarization is especially high where the intensity is high. So far, our results were obtained with w being 0. Lets' try some nonzero value!..]

---
w
Tuning w...
w = 0 meV
w = 6i meV
w = -6i meV
w = -4 meV
w = 2 - 2i meV
10
10
80
80
[Speaker Notes: As you can see, mechanical deformation also deforms the diffraction pattern. For real values of w, it stretches along the x axis, and it will be skew for imaginary values. Nevertheless, the pattern's topology does not change, which means that it's stable against such perturbation of the Hamiltonian. For w = 6i meV, the rays in k-space are present in the upper figure. To have an idea how the pattern further develops with changing w, let us map the complex plane of w to the 2D coordinate space of the focus' position!..]

---
map
The position of the focus as the function of w
The distortion of the lattice is ≤1% on this map.
[1] M. Mucha-Kruczyński, Phys. Rev. B 84, 041404 (2011)
[4] Gy. Dávid, Phys. Rev. B 85, 041402(R) (2012)
2 Dirac cones + 1 local min.
4 Dirac cones
2 Dirac cones
[Speaker Notes: For a given complex value of w in the curvy coordinate system, this map gives the location of the focal point in the (x,y) coordinate system. It can also be shown exactly that only a complex valued w can break the symmetry and shift the focus to the upper or lower plane, that is the Re(w) axis coincides with the x axis. The green and red thick lines divide regions of the low-energy band structure with a different topology. [A1] Inside the green region (including the zero w case), 4 Dirac cones touch the Fermi surface, in between the green and red lines, we find only 2 Dirac cones with a Berry's phase of 'p, and two other cones merged together into a local minimum with zero Berry's phase, and finally, in the outer region there are only two Dirac cones without any local minimum. In this map, the lattice distortion is less than 1% everywhere. When we neglect the interlayer shear shift, [a simple relation] can be found between w and [the strain tensor]. Here 'h is a real constant describing mechanical properties of the lattice, 'd>'d’ are the principal values of the [strain tensor] and 'q is the angle between the principal axes and coordinate axes (x, y). // In the strain tensor, i and j are the (x, y) coordinate-indexes and (dx , dy) denote displacements from the equilibrium positions. Thus, the imaginary phase of w is −2'q, reflecting a direct relation to the geometrical deformation of the lattice. //...a ‘hydrostatic’ rescaling of the lattice and only affects the values of m and v3. ... this effect on the diffraction pattern is negligible. // At every point in a stressed body there are at least three planes, called principal planes, with normal vectors n, called principal directions, where the corresponding stress vectors are parallel or in the same direction as the normal vector n, and where there are no normal shear stresses.]

---
fogak
w
w
w
w
w
w
w
w
w
[Speaker Notes: This grid of figures shows the dispersion surface of BLG with a few different values of w. [A1] Two of them are exactly there, sitting on the red or on the green line. By [this one] a local minimum has just disappeared by the crossing the red line, and by [this one] three Dirac points are merging together, and depending on how we move on in the complex plane of w, [this way] we get two Dirac points, and [this way] also an additional local minumum.]

---
Landau
Experimental relevance
β=0, Eν~(ν+½)
β=π, Eν~√ν
Landau levels at different filling factors5
[5] A. S. Mayorov et al., Science 333, 860 (2011)
[Speaker Notes: The investigation of the band structure's topology at low energies is taking place on the experimental field as well. Mayorov's paper presents results of Landau level measurements at different magnetic fields and filling factors. They found experimental evidence for the theoretical model, where the Dirac cones with Berry's phase 'p produce Landau levels proportional with '/'n, while a local minimum with zero Berry's phase produces Landau levels proportional with ('n+1/2).]

---
transparency
High transparency within the same band!
K’-electrons
K-electrons
When neglecting trigonal warping
Transmission probability as the function of . (w = 0 meV)
Ei = + 80 meV
Et = - 36 meV
Interband scattering
Ei = + 80 meV
Et = + 36 meV
Intraband scattering
[Speaker Notes: It is well known that negative refraction and focusing occurs in BLG also when a planar potential step induces scattering from the conduction band to the valence band or vice versa. However, there is a huge difference between interband and intraband scattering! While in the case of interband scattering the transmission probability has a maximum at 0.5 and it vanishes at perpendicular incidence (thus making the focus disappear!), [A1] intraband scattering proves to be highly transparent with a transmission probability close to 1, for electrons in both valleys!]

---
Summary
Summary
- Electronic Veselago lens in BLG with a planar potential step => Coherent focusing of electrons
- Trigonal warping => Anisotropy, negative refraction
- Valley selection => High degree of polarization
- Intraband scattering => High transparency
- Topology and symmetries of the low-energy band structure can be analysed
- Sensitive strain measurement
- Electron optical applications
[Speaker Notes: Now summarizing our results: We have proposed an electronic Veselago lens in BLG with a planar potential step, and showed that coherent focusing of electrons occurs. This is a consequence of the trigonal warping effect, which renders this electron optical system anisotropic, and results in negative refraction. The scattering proved to be valley selective, thus efficiently separating K and K' electrons in real space. Due to intraband scattering, the transmission probability of the incident electrons is very high, in contrast to the interband scattering process. Our proposal for an experimental setup can be applied to analyse the topology and symmetries of the low-energy band structure of BLG. Further applications may be possible in electron optics and strain measurement...]

---
Thank you
Thank you
for your attention.
[Speaker Notes: Mehettek ebédelni!]